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TS-09
(Non-Cementitious Advanced PolyAcrylic Waterproofing)







Make a primer by mixing TS-09 and water in the ratio of 1:5. Mix it well with the help of any stirrer so as to completely mix the chemical in water. Apply it with brush, roller of airless spray.
Take TS-09in a bucket and apply 2 coats of the chemical on the surface. If needed 10% water can be added to the chemical.

CONSUMPTION
Consumption varies from surface to surface. It is recommended to consume at least 0.6 - 0.7 ltr of TS-09 per 1m2 in 2 coats to form a thickness of approx 400 microns.



DESCRIPTION
TS-09 in itself is a complete waterproofing solution. It is low viscosity white coloured liquid which cures with humidity in atmosphere to produce highly elastic membrane with strong adhesion to many types of surface. It is based on 100% pure elastomeric hydrophobic PolyAcrylic which results in thermal and UV resistance properties. 

RECOMMENDED FOR
It can be applied on gypsum boards, cement boards, asbestos sheets, tiles, metal and concrete surface.
FEATURES & BENEFITS
Strong adhesive strength
It is highly elastomeric in nature having expansion ability of >100%.
It is UV Resistant. Doesn’t lose its properties even when exposed to weather.
Its low viscosity helps the chemical in penetrating the surface and sealing pores and capillaries in it. 
Non-toxic after full cure
Once cured, the film breathes so there is no accumulation of humidity under the coat.
APPLICATION PROCEDURE
Surface preparation plays an important role in any waterproofing. One needs to make sure that the surface is dirt, dust and oil free. Use electric blower to blow off dust from the surface. 

Technical Data


	Appearance
	White Liquid

	Solid Content
	43  ±  5%      (ASTM – D 1644-03)

	Specific Gravity 
	0.98  ±  0.5 (ASTM – D 1475-03)

	Curing Time
	Approx.48 hours (at 20ºC, 50% RH)  (ASTM C 4125)*

	Drying Time @ 25º C.
	Approx 3 hours (ASTM D 1640-03)

	Resistance to Temperature
	Approx. -20 ºC to +110 ºC

	Elongation Break
	> 250 % (ASTM – D 2370-98)

	Water Permeability
	almost zero 

	UV Resistance
	10,000 hrs. No deterioration or color fade. (ASTM D 822)

	Flash Point
	Non-flammable

	Chemical Resistance
	Good

	Insulation Properties
	Good

	Adhesion Strength N / mm²
	72.00 (ASTM – D 903-98)

	Pull Off Test N / mm²
	2.913 (BS 1881:part 207:1992)

	Water Vapor Transmission g / h - m²
	0.32 (ASTM E 96-095) 
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